## BOARD OF TECHNICAL EDUCATION

PORVORIM-GOA

April, 2012 Examinations

Programme: Shipbuilding Engg.

Subject: Welding in Shipconstruction-II(4337)

# Time Duration: 3 Hrs.                                                Max. Marks: 75

Instructions: 1) All Questions are compulsory.

2) Figures to the right indicate full marks.

3) Assume suitable additional data if required.

| Q.No.1. | Answer any five of the following Questions: | 5 x 3 = 15 |
| --- | --- | --- |
| a) | Differentiate between TIG and MIG welding process. |  |
| b) | What is carbon equivalent? What is its significance on weldability of metals? |  |
| c) | What is weld reliability? Explain in brief. |  |
| d) | Sketch a Double-Vee butt joint for joining plates of 35mm thickness, showing the details of joint. |  |
| e) | Explain the reasons for estimating welding cost. |  |
| f) | Explain the health hazards faced by welder, in brief. |  |
| Q.No.2. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | What type of power supply unit is used in TIG welding? What is the use of high frequency unit? Explain in brief. |  |
| b) | What is the necessity of Pre-heat and Post-heating of welded joints? |  |
| c) | Explain the steps involved in qualifying a welder for 4-G position welding. |  |
| Q.No.3. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | How does the welding of high carbon steels differ from that of medium and low carbon steels? Explain in detail any one method of welding mild steel plates 10mm thick. |  |
| b) | Discuss the weldability of Austenitic stainless steels. |  |
| c) | i) What precautions are taken for welding of Grey-cast Iron? |  |
|  | ii)What does Destructive tensile test reveal about a weldment? |  |
| Q.No.4. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Differentiate between Face-bend and Root-bend tests, with appropriate sketches. |  |
| b) | Outline the principle of Dye-penetrant test of welds. What type of defects are revealed? |  |
| c) | How long a 15mm fillet weld is required to weld the long side of an angle 150x80x15mm to a steel plate, using the side welds only, if the load is 10,000N and the allowable shear load per centimeter of 15mm fillet weld is 800N? |  |
| Q.No.5. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | A lap joint is to be produced in 12mm Mild steel plates with a 6mm electrode using a current of 250 amps at 30 volts. Calculate the cost of labour, cost of power and cost of electrode for welding 10 metre length. Use the following data. Welding speed-12m/hr Electrode consumption-0.6 Kg/metre Cost of Electrode – Rs. 120/kg Labour Cost – Rs 100/hr Power cost – Rs 20/KWh Efficiency of welding machine – 80% Operating factor – 0.6. | …..2/- |

-2-

| b) | Explain the characteristics of a good under-water welding process. |  |
| --- | --- | --- |
| c) | i)Explain the basic types of welds. ii)Explain the term operating-factor used for estimation of welding cost. |  |
| Q.No.6. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | With a neat sketch, explain the method of cladding of shafts. |  |
| b) | With suitable example explain the method of hard facing. |  |
| c) | State the safety precautions which should be taken for each of the following: - Storage of Acetylene cylinders - Using Gas pressure regulators. |  |

***********