## BOARD OF TECHNICAL EDUCATION

PORVORIM-GOA

April, 2013 Examinations

Programme: Fabrication Technology & Erection Engg.

Subject: Materials & Processes(4238)

# Time Duration: 3 Hrs.                                               Max. Marks:  75

Instructions: 1) All Questions are compulsory.

2) Figures to the right indicate full marks.

3) Assume suitable additional data if required.

| Q.No.1. | Answer any five of the following Questions: | 5 x 3 = 15 |
| --- | --- | --- |
| a) | What is a martensite? Also explain the martensitic transformation process. |  |
| b) | Explain Heat Resisting steels. |  |
| c) | Explain any one process of identifying percentage constituents of elements in steel. |  |
| d) | Discuss the temperature distribution around the weld metal. |  |
| e) | Explain the concept of competitive growth in weld metal solidification. |  |
| f) | Explain the effect of heating time and cooling time on the properties of steel. |  |
| g) | Explain the significance of Recrystallisation temperature. |  |
| h) | Differentiate between thermoplastic and thermosetting plastic. |  |
| Q.No.2. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Explain the influence of Carbon, Manganese, Silicon, Sulphur and Phosphorus on the properties of steel. |  |
| b) | Distinguish between Austenitic, Martensitic and Ferritic type of stainless steel. |  |
| c) | Discuss Chilled cast iron and Alloy cast Iron. |  |
| Q.No.3. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Explain with a neat sketch the charpy impact test. |  |
| b) | What are the various methods used to relieve the internal stresses before and after welding? |  |
| c) | What is corrosion in welds? List down the various factors affecting corrosion. Also discuss the remedies to prevent corrosion. |  |
| Q.No.4. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Explain the process of Normalising with a sketch. |  |
| b) | Discuss the effect of quenching rate, grain size, composition of steel and alloying elements on the hardenability of steel. |  |
| c) | Explain the process of Age Hardening of a Al-Zn alloy. |  |
| Q.No.5. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Discuss the hot working and cold working of steels. Also discuss the need for process Annealing with regard to the cold working of steel. |  |
| b) | Discuss the process of strain hardening with its practical application. |  |
| c) | Discuss the effect of various gases on the structure of weld. Also explain hydrogen induced crack. |  |

………2/-

-2-

| Q.No.6. | Write short notes on any four: | 4 x 3 = 12 |
| --- | --- | --- |
| a) | Solid Solution |  |
| b) | Alloy Structural Steel |  |
| c) | Weld Decay |  |
| d) | L.D. Process for steel |  |
| e) | Polymers |  |
| f) | Full Annealing |  |

***********