## BOARD OF TECHNICAL EDUCATION

PORVORIM-GOA

April, 2015 Examinations

Programme: Mechanical Engg.

Subject: Tool Engineering-II[Press Tools] (5077)

# Time Duration: 3 Hrs.                                               Max. Marks:  75

Instructions: 1) All Questions are compulsory.

2) Figures to the right indicate full marks.

3) Assume suitable additional data if required.

| Q.No.1. | Design and draw a die to produce the sheet metal part shown in fig.1. The sheet material is steel with ultimate tensile strength 420 N/mm2. The design must include: i) Press tonnage calculation ii) Economic strip layout iii) Bill of material. Draw at least two views. | (40) |
| --- | --- | --- |
| Q.No.2. | Answer any two of the following Questions: | 2x10=20 |
| a) | i) What is meant by press tonnage? ii) How is tonnage of hydraulic press determined? iii) How is tonnage of mechanical press determined? iv) What is shut height of press? v) What is the purpose of strippers in punch and die operations? |  |
| b) | i) Classify the different types of shearing operations and explain briefly. ii) Explain Bending methods with sketches. |  |
| c) | i) What is meant by ironing when discussing drawing operation? ii) Explain the importance of strip layout and how is it carried out. |  |
| Q.No.3. | Write short notes on any three: | 3 x 5 = 15 |
| a) | Rubber dies |  |
| b) | Stretch forming |  |
| c) | Horn type dies |  |
| d) | Progressive dies |  |
| e) | Springback effect |  |