## BOARD OF TECHNICAL EDUCATION

PORVORIM-GOA

November, 2014 Examinations

Programme: Shipbuilding Engg.

Subject: Welding In Shipconstruction-II(4337)

# Time Duration: 3 Hrs.                                               Max. Marks:  75

Instructions: 1) All Questions are compulsory.

2) Figures to the right indicate full marks.

3) Assume suitable additional data if required.

| Q.No.1. | Answer any five of the following Questions: | 5 x 3 = 15 |
| --- | --- | --- |
| a) | What is importance of Jigs and fixtures during welding? |  |
| b) | How is welding of Aluminum different from that of welding steel? |  |
| c) | Write a short note on any leak test carried on weldment. |  |
| d) | What are the important factors considered for a good weld joint design? |  |
| e) | Give the various factors affecting welding costs. |  |
| f) | Distinguish between metal spraying and hard facing. |  |
| Q.No.2. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Which parts of the ship are considered for submerged arc welding? Describe the welding process with a neat sketch. |  |
| b) | Explain the TIG welding process. Give a few applications of the same in ship construction. |  |
| c) | Explain the importance of Pre and Post heat treatments of welds. |  |
| Q.No.3. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Describe the welding of dissimilar metals. |  |
| b) | Describe welding of Ferritic or Martensitic stainless steels. |  |
| c) | Explain dye penetrant testing of weldment. |  |
| Q.No.4. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | List the destructive tests of weldment and explain any one in detail. |  |
| b) | Calculate the total costs of manual flux shielded metal arc welding using data given below: Weld length = 3 m Weld speed = 13 m/hr Operating factor = 30% Labour and overhead = Rs. 200/- Charges per hour Electrode consumption = 0.35 Kg/m Electrode Price = Rs. 250 per Kg Arc Voltage = 22 volts Arc Current = 200 Amps E = 0.6 Rate per KWhr = Rs. 5 |  |
| c) | Explain the classification society requirement for welding in ship construction activity. |  |
| Q.No.5. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Describe the under water welding process in detail. |  |
| b) | Name some ship components which need cladding to be done. How is the cladding process carried out? |  |
| c) | Summarize the safe working practices in welding. |  |
|  |  | ……2/- |
|  | -2- |  |
| Q.No.6. | Write short notes on any three: | 3 x 4 = 12 |
| a) | Welder’s performance qualification |  |
| b) | Welding positions |  |
| c) | Reconditioning Machine parts |  |
| d) | Health of Welders |  |

***********