## BOARD OF TECHNICAL EDUCATION

PORVORIM-GOA

November, 2014 Examinations

Programme: Fabrication Technology & Erection Engg.

Subject: Welding Technology-I(4237)/(FE301) [Old/Revised]

# Time Duration: 3 Hrs.                                               Max. Marks:  75

Instructions: 1) All Questions are compulsory.

2) Figures to the right indicate full marks.

3) Assume suitable additional data if required.

| Q.No.1. | Answer any five of the following Questions: | 5 x 3 = 15 |
| --- | --- | --- |
| a) | Explain the advantages of welding as a Fabrication process over other joining processes. |  |
| b) | What is Back Gouging and Filling? When and why is it required? |  |
| c) | Explain why, copper piping is not to be used in Acetylene Manifolding system. |  |
| d) | List the different types of Electrodes used in different arc welding processes. |  |
| e) | Differentiate between Welding and Brazing as joining processes. Mention any two advantages of Brazing over Welding. |  |
| f) | What is Metal spraying? List its applications. |  |
| g) | Explain why, medium carbon steel is more difficult to weld than structural steel. |  |
| Q.No.2. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Explain the following terms in welding: i) Molten puddle ii) Heat Affected Zone iii) Heat Input iv) Penetration v) Distortion vi) Weld contamination. |  |
| b) | Explain the advantages of Gas Manifolding system. Differentiate between Acetylene and Oxygen gas manifolding systems. |  |
| c) | Explain the procedure to set, light, adjust, use and extinguish the oxy-acetylene flame welding equipment. |  |
| Q.No.3. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Explain with a neat sketch the construction and working of an air-acetylene flame welding Torch. |  |
| b) | With a neat sketch explain the structure and mechanism of a Welding Arc. |  |
| c) | Differentiate between Drooping and Flat power source characteristics with neat sketches. Mention the type of Power source characteristic used for MMAW and Why. |  |
| Q.No.4. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Explain the different types of cracking in welds. Explain the causes and remedies of hot and cold weld cracking. |  |
| b) | Explain the procedure to perform Brazing and Soldering. |  |
| c) | Explain the objectives of Hardfacing of steel. Explain the procedure to perform Hardfacing. |  |
| Q.No.5. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Explain the harmful effects of welding arc on the operator and explain how they are taken care of. |  |
| b) | Explain oxy-acetylene flame welding of Grey Cast Iron. |  |
| c) | Explain why, not all stainless steels are weldable. | ……..2/- |
|  | -2- |  |
| Q.No.6. | Write notes on any three: | 3 x 4 = 12 |
| a) | Acetylene Gas Generator |  |
| b) | Low Hydrogen Electrodes |  |
| c) | Importance of Joint cleanliness in Brazing |  |
| d) | Welding of Nickel and its Alloys |  |
| e) | Brazing Alloys |  |

***********